## Slide 1: Vehicle Surface Preparation and Masking
Chapter 25
Notes: 1

## Slide 2
FIGURE 25–1 After sheetmetal work is done, a vehicle is moved to the surface prep/masking area.

## Slide 3: Objectives
Determine whether an existing finish is defect free and adheres soundly to a vehicle
Select the correct abrasive and sanding techniques for specific final sanding operations
Prepare existing paint films and bare metal substrates for refinishing
Describe the three methods of removing a deteriorated paint film
Notes: 3

## Slide 4: Objectives (continued)
Determine when to apply a primer, a primer-sealer, a primer-surfacer, or glazing putty
Prepare plastic parts for refinishing
Mask a car, panel, or spot repair for refinishing
Comply with EPA rules
Correctly answer ASE-style review questions relating to vehicle surface preparation and masking

## Slide 5: Introduction
Surface preparation
  Getting body surface clean, smooth, primed, puttied, sanded, scuffed, and wiped clean to ready it for painting
Proper surface preparation is the foundation of a good paint job
Notes: 5

## Slide 6: Evaluate Surface Condition
Vehicle surface evaluation
  Determine what must be done before painting body surface
  Check gloss level, adhesion and surface rust
Checking paint thickness
  Measured in mils, or thousandths of an inch (hundredths of a millimeter)
  Original OEM paints: about 3 to 6 mils thick
  Paint buildup should be limited to no more than 12 to 14 mils

## Slide 7: Evaluate Surface Condition (continued)
Checking paint thickness (continued)
  Mil gauge, also called paint thickness gauge, can be used to measure thickness of paint
    Pencil mil gauge
    Electronic mil gauge

## Slide 8
FIGURE 25–5 (A) A Tinsley gauge, also called a pencil mil gauge, is an inexpensive but effective way to check paint thickness in three steps. (B) By pulling the gauge, a magnet will stick to a steel body but will not work on aluminum or plastic panels. Thicker paint will allow you to pull the tool off the vehicle body with less effort.

## Slide 9: Paint Removal
Three common ways to strip paint from metal surfaces
  Chemical stripping
  Media blasting
  Sanding or grinding
Chemical paint removal
  Chemical paint remover can be used for stripping large areas of paint if environmental regulations allow
    No danger of metal warping

## Slide 10: Paint Removal (continued)
Blasting off paint
  Blasters: air-powered tools for forcing sand, plastic beads, or another abrasive onto surfaces for paint removal
    Preferred when trying to remove surface rust
Types of media blasters
  Pressure blasters
  Siphon blasters

## Slide 11
FIGURE 25–7 Media blasting is a fast and effective way to remove paint from smaller areas.

## Slide 12: Paint Removal (continued)
Types of blasting media
  Plastic media blasting
  Sand blasting
  Soda blasting
Using a blaster
  Basic procedure for operating a blaster:
    Mask off areas that will not be affected by spot repair
    Put on necessary safety gear

## Slide 13: Paint Removal (continued)
Using a blaster (continued)
    Before blasting, check manufacturer’s instructions for proper blasting pressures, sand load procedures, and setup arrangements
    When ready to blast, apply abrasive material directly onto area to be blasted; when area shows no brown rust, remove pressure
    Watch surface carefully
    After paint is removed, use air blowgun to remove sand from all areas of vehicle
    Prime metal as soon as possible after any stripping process

## Slide 14: Paint Removal (continued)
Sanding off paint
  Orbital sanding with flexible backing pad is suitable for removing old finish from small flat areas and gently curved areas

## Slide 15: Preparing Bare Metal
Proper preparation of bare metal is a critical step in restoring vehicle to its preaccident condition
Using metal conditioners
  Metal conditioner: acid-type chemical wash that eats away any material that might prevent good primer-to-metal bond
    Wipe-on metal conditioners are seldom used today
    Might be used when surface rust could pose a problem

## Slide 16: Preparing Bare Metal (continued)
Preparing hard chrome surfaces
  Clean metal with wax-and-grease remover
  Thoroughly sand metal
  Reclean with wax-and-grease remover
  Apply metal treatment
  Spray two coats of primer-surfacer; allow adequate drying time before dry sanding
  Blow out cracks, then use a tack cloth on entire surface; final coat can then be applied

## Slide 17: Preparing Bare Metal (continued)
Preparing metal replacement parts
  Shipping coating: protects metal against corrosion and rust during storage and shipping
  E-coat: paintable primer that is an essential part of factory corrosion protection warranty on new factory panels and parts
Using self-etch primer
  Self-etch primers chemically eat into bare metal to improve paint adhesion and corrosion resistance while also priming the surface

## Slide 18: Preparing Bare Metal (continued)
Apply seam sealer
  Seam sealer: needed anywhere water leakage might be a problem between panel joints—often on welded panels forming passenger compartment and trunk areas

## Slide 19
FIGURE 25–12 In the prep area, you must also check for correct application of seam sealer. (A) The sheetmetal technician forgot to apply seam sealer here. If the vehicle had been painted and leaked, the painter might have had to repaint the vehicle for free. (B) Use a small brush to smoothly spread seam sealer. You want it to look like the original OEM sealer. Brushing will also improve bonding of sealer.

## Slide 20: Primecoat Selection
Decision to apply primer, primer-sealer, adhesion promoter, or primer-surfacer depends on the following three factors
  Condition of substrate: smooth or rough, bare or painted
  Type of finish on substrate if painted
  Type of finish to be used for topcoat

## Slide 21: Primecoat Selection (continued)
Applying primecoats
  Reduce primecoat chosen according to manufacturer’s instructions
  Select proper solvent for the weather conditions and thoroughly mix the material
  Generally, only one or two coats of primer or primer-sealer are required
  Primer-surfacer and primer-filler also require one or two coats for proper buildup

## Slide 22: Primecoat Selection (continued)
Applying spot putty
  Once primer is dry, any remaining small pinholes and scratches must be filled with spot putty, or glazing putty

## Slide 23
FIGURE 25–17 Note how different layers of repair materials are often applied during panel repair.

## Slide 24: Final Sanding
Involves using fine and very fine grits of material to prepare body surfaces for painting
Entire surface to be refinished must be scuff sanded to improve adhesion of new paint
Use the right grit
  Correct grit or sandpaper coarseness
    Lower the number on the back of the sandpaper, coarser the grit
    Start work with coarsest grit practical
    Gradually go to finer paper to achieve desired surface smoothness

## Slide 25: Final Sanding (continued)
Surface sanding methods
  Refinishing sanding can be done by hand or by using power equipment
Power sanding
  Orbital sander, or DA sander, moves in two directions at the same time
    Produces much smoother surface finish
    Used to featheredge repair area and to final sand larger panel areas

## Slide 26: Final Sanding (continued)
Hand sanding
  Simple back and forth scrubbing action with sandpaper flat against the surface
  Can be done with your fingers on sharply curved surfaces
  On flat or large curves use sanding block to support sandpaper
Dry sanding
Wet sanding

## Slide 27
FIGURE 25–28 Generally, sand with the body lines of a panel. This will speed your work and help to prevent paint runs on the side of the vehicle.

## Slide 28
FIGURE 25–31 When final wet sanding flat or gently curved surfaces, use a sanding block. The block will help plane down and level minor surface imperfections much better than just using your hand.

## Slide 29: Final Sanding (continued)
Surface scuffing
  Using very fine or ultrafine abrasive (paste material, sandpaper, or scuff pad) to cut microscopic scratches in the body surface to be painted
    Finely scratches surface to aid proper paint adhesion

## Slide 30: Masking
Keeps paint from contacting areas that are not meant to be refinished or painted
Four basic ways to mask
  With masking paper and masking tape
  With plastic sheeting and masking tape
  With specially shaped cloth or plastic covers (for wheels, antenna, and rearview mirrors)
  With liquid masking material

## Slide 31
FIGURE 25–38 Masking materials are used to cover panels and parts that will not be painted.

## Slide 32: Masking (continued)
Clean before masking
  Before any types of masking materials are applied, vehicle must be completely cleaned and all dust blown away
Liquid masking material
  Seals off large, complex surfaces of vehicle to protect them from paint overspray
  Used on areas such as wheel wells, headlights, grille, underbody chassis, engine compartment, etc.

## Slide 33
FIGURE 25–40 Liquid masking material is often used on large surfaces that will not be painted. After painting, liquid mask material washes off with soap and water or with a pressure washer. Here a spray-on mask is being applied to the engine compartment to protect the engine and other parts from overspray.

## Slide 34: Masking (continued)
Plastic sheet masking
  Very thin clear plastic that can be used to cover and protect large body surfaces from overspray
Masking paper and tape
  Use correct type of masking paper as recommended by the manufacturer
  Primer masking paper
  Paint masking paper

## Slide 35
FIGURE 25–42 The masking paper should lap over the plastic. Tape the plastic to the body and then the paper to the plastic.

## Slide 36: Masking (continued)
Masking paper and tape (continued)
  Masking tape: very sticky paper tape designed to cover small parts and also to hold masking paper in place
  Fine line masking tape
Masking versus removing a part
  Decision to remove or mask depends on the design of vehicle, insurance company stipulations, and expectations of the customer
Decal and tape stripe removal

## Slide 37: Masking (continued)
Applying masking tape and paper
  Blow and wipe parts off before masking them to ensure good tape adhesion
  When applying masking tape:
    Hold and peel tape with one hand
    Use your other hand to guide and secure tape to vehicle
  Tape down all loose paper and plastic, and large areas of masking paper
    Tape along the bottom of vehicle to hold paper on the bottom of the body

## Slide 38
FIGURE 25–52 Make sure loose masking paper cannot flop and hit wet paint. Airflow from a spray gun can make loose paper blow around. Tape around or over all loose ends.

## Slide 39: Masking (continued)
Applying masking tape and paper (continued)
  Masking leak problem
  Overmask and undermask problem
  Double masking
Masking aids
  Wheel masks: preshaped plastic or cloth covers that fit over vehicle’s wheels and tires
  Preshaped plastic antenna, headlamp, and mirror covers

## Slide 40: Masking (continued)
Masking panel gaps
  Back masking: applying tape to the rear or inside edges of panels so that only front of panel is painted
  To back mask a panel gap:
    Apply tape along the back of panel so that tape sticks out enough to cover the gap between adjacent panels
    Close door or hood and push tape back into part gap

## Slide 41: Masking (continued)
Masking openings
  Masking openings in panels
  Masking wheels and wheel openings
  Masking hood or trunk lid
  Masking door openings
Reverse masking
  Done by rolling tape over and into a curved shape to prevent visible paint parting line along masking tape
Masking rope

## Slide 42
FIGURE 25–56 Note the two methods for masking a wheel opening. (A) Because only the rear bumper is to be painted, the whole wheel opening did not have to be fully masked. (B) Full wheel opening masking is needed when painting the panel area over or around the opening.

## Slide 43: Surface Cleaning
Before pulling vehicle into paint booth, blow it off again
Remove contaminants, especially tar and grease, from surface before final sanding
Clean surface again right before painting
  Oil from air tools or your hands can contaminate vehicle surface and cause problems when spraying on topcoats

## Slide 44: Surface Cleaning (continued)
Using wax-and-grease remover
  Before and after sanding, use wax-and-grease remover or recommended solvent to thoroughly clean the surface
  Maximum effectiveness is achieved by wiping up wax-and-grease remover while it is still wet
  To remove any last trace of moisture and dirt from seals and moldings, blow them out with compressed air at low pressure
  Always include some wax-and-grease cleaner or detergent in sanding water

## Slide 45
FIGURE 25–71 After surface preparation, the vehicle should again be wiped down with wax-and-grease remover. Use one clean rag to apply the cleaning agent. Use another dry rag to wipe the cleaner off right away before it dries.

## Slide 46: Summary
The term surface preparation refers to getting a vehicle’s surface clean, smooth, and ready for the application of the final colorcoats.
A dull primer surface may look smooth and ready for paint to the untrained eye. You must remember that the paint will actually work like a magnifying glass to exaggerate any scratches or irregularities.
Before painting, you should identify the type of paint and overall condition of the existing paint system.

## Slide 47: Summary
Paint thickness is measured in mils or thousandths of an inch. OEM paints are typically about 3–6 mils thick.
Blasters are air-powered tools for forcing sand, plastic beads, or another material onto surfaces for paint removal. A chemical paint remover can also be used for stripping large areas of paint if environmental regulations allow.
Sanding uses an abrasive-coated paper or plastic backing to level and smooth a body surface.

## Slide 48: Summary
Grit sizes vary from coarse to ultrafine grades and are rated by number.
Power grinding is done to quickly remove large amounts of old paint and other materials.
When sanding, make sure you are using the correct grit number for the job.
An orbital sander or DA sander moves in two directions at the same time, an action that produces a much smoother surface finish.

## Slide 49: Summary
Scuff sanding removes any trace of contaminants on the existing finish and textures the surface so paint will adhere properly.
If the primer-surfacer is sanded before all of the solvent has evaporated, the material in the scratches will continue to shrink down in the scratches.
After the primecoat is dry, block sand the area until it is smooth.
A guide coat helps to point out unlevel surface areas.

## Slide 50: Summary
Once the primer is dry, small pinholes and scratches can be filled with spot putty or glazing putty.
Masking keeps paint from contacting areas other than those to be refinished or painted.
Automotive masking paper is heat-resistant so that it can be used safely in baking ovens.
Liquid masking material seals off the entire vehicle to protect undamaged panels and parts from paint overspray.

## Slide 51: Summary
Masking tape is very sticky paper tape designed to cover small parts and also to hold the masking paper in place.
Fine line masking tape is a very thin, smooth-surface plastic masking tape.
Masking covers are specially shaped cloth or plastic covers for masking specific parts.